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Section 04 73 00
manufactured masonry veneer

	
GENERAL NOTES TO SPECIFIER:

THIS SPECIFICATION SECTION HAS BEEN PREPARED TO ASSIST DESIGN PROFESSIONALS IN THE PREPARATION OF PROJECT OR OFFICE MASTER SPECIFICATIONS. IT FOLLOWS GUIDELINES ESTABLISHED BY THE CONSTRUCTION SPECIFICATIONS INSTITUTE (CSI), AND THEREFORE MAY BE USED WITH MOST MASTER SPECIFICATION SYSTEMS WITH MINOR EDITING.

EDIT CAREFULLY TO SUIT PROJECT REQUIREMENTS. MODIFY AS NECESSARY AND DELETE ITEMS THAT ARE NOT APPLICABLE. VERIFY THAT REFERENCED SECTION NUMBERS AND TITLES ARE CORRECT. (NUMBERS AND TITLES REFERENCED ARE BASED ON MASTERFORMAT, 2004 EDITION).

THIS SECTION ASSUMES THE PROJECT MANUAL WILL CONTAIN COMPLETE DIVISION 1 DOCUMENTS INCLUDING 
SECTIONS 01 25 13PRODUCT SUBSTITUTION PROCEDURES, 01 33 00SUBMITTAL PROCEDURES, 01 62 00PRODUCT OPTIONS, 01 66 00PRODUCT STORAGE AND HANDLING REQUIREMENTS, 01 74 00cLEANING and waste management, 01 77 00CLOSEOUT PROCEDURES, AND 01 78 00CLOSEOUT SUBMITTALS. CLOSE COORDINATION WITH DIVISION 1 SECTIONS IS REQUIRED. IF THE PROJECT MANUAL DOES NOT CONTAIN THESE SECTIONS, ADDITIONAL INFORMATION SHOULD BE INCLUDED UNDER THE APPROPRIATE ARTICLES.

THIS IS A CLOSED PROPRIETARY SPECIFICATION.

NOTES TO THE SPECIFIER ARE CONTAINED IN BOXES AND SHOULD BE DELETED FROM FINAL COPY.

GREY HIGHLIGHTED GREEN TEXT AND NOTES RELATE TO LEED® PROJECTS AND CAN BE DELETED IF THE PROJECT IS NOT INTENDED TO ATTAIN leed® CERTIFICATION. Credit references refer to leed® for new construction, v2.2.

OPTIONAL ITEMS REQUIRING SELECTION BY THE SPECIFIER ARE ENCLOSED WITHIN BRACKETS, E.G. [35] [40] [45]. MAKE APPROPRIATE SELECTIONS AND DELETE OTHERS.

ITEMS REQUIRING ADDITIONAL INFORMATION ARE UNDERLINED BLANK SPACES, E.G.  ___________ .

OPTIONAL PARAGRAPHS REQUIRING SELECTION OF ONE OF THE OPTIONS ARE SEPARATED BY “OR” WITHIN A BOX, E.G.
OR

BOLD FACE text IDENTIFIES OPTIONAL PARAGRAPHS AND FEATURES THAT MAY BE INCLUDED OR DELETED DEPENDING ON PROJECT REQUIREMENTS. CONVERT THE BOLD FACE Text TO REGULAR Text WHEN INCLUDING THESE PARAGRAPHS OR FEATURES. WHEN DELETING A PARAGRAPH, BE CERTAIN THAT ALL SUBPARAGRAPHS ARE ALSO DELETED.

revise footer to suit project/office requirements.

ELECTRONIC VERSIONS OF THIS SPECIFICATION UTILIZE AUTOMATIC PARAGRAPH NUMBERING.








General
Summary
Section Includes: Portland cement based manufactured [stone] [and] [brick] veneer and trim.
Related Sections: 
INCLUDE ALL DIVISION 01 SECTIONS CONTAINING LEED® REQUIREMENTS.
__ __ _____________________. Wall Framing.
__ __ _____________________. Wall Sheathing.
07 60 00Flashing and Sheet Metal.
07 92 00Joint Sealants.
09 24 00–Portland Cement Plastering.
10 30 00Fireplaces and Stoves.
INCLUDE APPROPRIATE LANGUAGE BELOW IF PRODUCTS SPECIFIED IN THIS SECTION ARE TO BE BID AS ALTERNATES. OTHERWISE DELETE FOLLOWING PARAGRAPH.
Alternates:
Reference Section 01 23 00Alternates.
References 
American National Standards Institute (ANSI):
ANSI A118.4 Specifications for Latex-Portland Cement Mortar.
ANSI A118.15 – American National Standard Specification for Improved Modified Dry-Set Cement Mortar
American Society for Testing and Materials (ASTM):
ASTM C140/C140M – Standard Test Method for Sampling and Testing Concrete Masonry Units and Related Units 
ASTM C270 – Standard Specification for Mortar for Unit Masonry.
ASTM C847 – Standard Specification for Metal Lath 
ASTM C933 – Standard Specification for Welded Wire Lath 
ASTM C1670/C1670M – Standard Specification for Adhered Manufactured Stone Masonry Veneer Units 
ASTM C1714/C1714M – Standard Specification for Preblended Dry Mortar Mix for Unit Masonry 
ASTM C1780 – Standard Practice for Installation Methods for Cement-Based Adhered Masonry Veneer 
ASTM D226/D226M – Standard Specification for Asphalt-Saturated Organic Felt Used in Roofing and Waterproofing 
ASTM E2556/E2556M – Standard Specification for vapor Permeable Flexible Sheet Water-Resistive Barriers Intended for Mechanical Attachment 
ICC AC38 Acceptance Criteria for Water Resistive Barriers
City of Los Angeles: Research Report (LARR)
Research Report #25589
International Code Council (ICC):
ESR Report.
LEED®: US Green Building Council’s Leadership in Energy and Environmental Design Green Building Rating System™.
Underwriter's Laboratory (UL): Building Materials Directory.
US Department of Housing and Urban Development (HUD): Material Release Numbers 910Fs.
Submittals
Reference Section 01 33 00Submittal Procedures; submit following items:
Product Data.
Samples:
Standard sample board consisting of small-scale pieces of veneer units showing full range of textures and colors.
Full range of mortar colors.
Verification Samples: Following initial sample selection submit “laid-up” sample board using the selected stone and mortar materials and showing the full range of colors expected in the finished Work; minimum sample size: 3 by 3 feet (1 by 1 m).
Quality Assurance/Control Submittals:
Qualifications: 
Proof of manufacturer qualifications.
Proof of installer qualifications.
Regulatory Requirements: Evaluation reports.
Veneer manufacturer’s installation instructions.
Installation instructions for other materials.
LEED® Submittals:
Credit MR 4.1, 4.2 Recycled Content: Provide percentage of recycled content (post- consumer and pre-consumer).
Credit MR 5.1, 5.2 Regional Materials:
Provide distance between Project site and extraction site.
Provide distance between Project site and final manufacturing location.
MANUFACTURED MASONRY CAN ALSO CONTRIBUTE TO CREDIT EA 1 FOR OPTIMIZING ENERGY PERFORMANCE AND CREDITS ID 1.1-1.4 FOR INNOVATION IN DESIGN, HOWEVER, NO SPECIFIC SUBMITTALS ARE REQUIRED IN THIS SECTION.
Closeout Submittals: Reference Section 01 78 00Closeout Submittals; submit following items:
Maintenance Instructions.
Special Warranties.
Quality Assurance
Qualifications:
Manufacturer Qualifications: Eldorado Stone, LLC.
Installer Qualifications: Experienced mason familiar with installation procedures and related local, state and federal codes masonry. 
Certifications:
ICC Evaluation Service  Evaluation Report ESR-1215.
ICC ESR-1215, Florida Building Code Supplement
ASTM C1670
LARR – Research Report RR25589
HUD  Material Release Number 910F
UL  Classification listing in Building Materials Directory: UL 546T (F8002).
Field Sample:
COMPLETE FOLLOWING SUBPARAGRAPH TO INCLUDE DESIRED DETAILS SUCH AS CORNERS, TRIM, MORTAR JOINTS AND JOINT DETAILS ABUTTING OTHER MATERIALS.
Prepare [4 by 4 foot (1200 by 1200 mm)] [ __ by __ foot ( ____ by ____ mm)] sample at a location on the structure as selected by the Architect. Use approved selection sample materials and colors. Include _______________________________________.
Obtain Architect’s approval.
Protect and retain sample as a basis for approval of completed manufactured stone work. Approved sample may be incorporated into completed work.
Delivery, Storage, and Handling
Reference Section 01 66 00Product Storage and Handling Requirements.
Follow manufacturer’s instructions.
Project/SITE Conditions 
Environmental Requirements: When air temperature is 40 degrees F (4.5 degrees C) or below, consult local building code for Cold-Weather Construction requirements.
Warranty
Special Warranty: Manufacturer’s standard warranty coverage against defects in materials when installed in accordance with manufacturer’s installation instructions.
Products
Manufacturer
Acceptable Manufacturer: Eldorado Stone®, which is located at: 3817 Ocean Ranch Boulevard, Ste 114, Oceanside, CA 92056; Toll Free Tel: (800) 925-1491; Email to request info: cs@westlake.com; Web: www.eldoradostone.com
Product: [_________________ veneer] [Veneer types as shown on Drawings].
Substitutions: Not permitted. 
Requests for substitutions will be considered in accordance with provisions of Section 01 60 00 – Product Requirements.
INSERT NAME, ADDRESS AND CONTACT INFORMATION OF LOCAL DISTRIBUTOR BELOW.
Manufacturer’s Distributor:
Materials
Stone Veneer & Brick Veneer:
SELECT DESIRED PROFILE FROM THE ELDORADO STONE WEBSITE PRODUCTS PAGE; INSERT PROFILE AND COLOR SPECIFICATION BELOW.
Profile: __________________________. Include matching corner pieces.
Color: ___________________________.
SELECT DESIRED STONE ACESSORIES FROM THE ELDORADO STONE WEBSITE ACCESSORIES PAGE; INSERT DESIRED ACCESSORIES BELOW AND INSERT TEXTURE IF REQUIRED. VERIFY THAT DIMENSIONS, IF REQUIRED, ARE SHOWN ON THE DRAWINGS.
Accessories
Stone Accessories: ___________________________.
Color: ___________________________.
Execution
Examination
Examine substrates upon which work will be installed.
Coordinate with responsible entity to perform corrective work on unsatisfactory substrates.
Commencement of work by installer is acceptance of substrate.
Preparation
Protection: Protect adjacent work from contact with mortar.
Surface Preparation: Prepare substrate in accordance with manufacturer’s installation instructions for the type of substrate being covered.
INSTALLATION
Install and clean stone in accordance with manufacturer’s installation instructions for Standard Installation (Grouted Joint) or Jointless/Dry-Stacked installation as specified above.
Apply repellent in accordance with repellent manufacturer’s application instructions.
Field Quality Control
Manufacturer's Field Services: Request a Manufacturer’s Field Service Representative site visits for pre-construction meeting to review installation guidelines.  
Cleaning
Reference Section 01 74 00Cleaning and Waste Management.
Remove protective coverings from adjacent work.
Cleaning Veneer Units:
Wash with soft bristle brush and water/granulated detergent solution
Rinse immediately with clean water
Removing Efflorescence:
Allow veneer to dry thoroughly
Scrub with soft bristle brush and clean water
Rinse immediately with clean water; allow to dry
If efflorescence is still visible, contact Eldorado Stone Customer Service for assistance


End of Section[footnoteRef:1] [1:  	This specification was prepared specifically for Eldorado Stone Corporation by ASC Specification Consultants. Comments or suggestions for improvement should be addressed to Eldorado Stone via the contact information on page one.
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